## Slide 1: Assessing DFT+U methods and associated corrections to describe lanthanide-doped, large band gap oxides
Dan Criveanu

## Slide 2: Quantum computers can make many currently infeasible problems feasible

## Slide 3: Quantum computers can make many currently infeasible problems feasible

## Slide 4: Quantum computers can make many currently infeasible problems feasible

## Slide 5: Quantum computers can make many currently infeasible problems feasible

## Slide 6: New materials need to be discovered for quantum computing
Stability
Quantum computers currently have problems with:
Scalability
Qubits are kept at 15 millikelvin in a dilution refrigerator.
Current qubit limit is 54. We need thousands.
Notes: Stability – IBM’s quantum computers need to be kept at very low temperatures (15 millikelvin in a dilution refrigerator).
Scalability – currently having too many qubits will lead to the qubits deactivating each other.

## Slide 7: Potential solution: Lanthanide dopants in wide band gap oxides
d/f
s/p
f- (and d-) orbitals are highly localised

## Slide 8: Potential solution: Lanthanide dopants in wide band gap oxides
Valence band
Conduction band
E
Ln 5d (empty)
Ln 4f (filled)
d/f
s/p
Ln dopant in a wide band gap host
f- (and d-) orbitals are highly localised

## Slide 9: Potential solution: Lanthanide dopants in wide band gap oxides
Valence band
Conduction band
E
Ln 5d (empty)
Ln 4f (filled)
d/f
s/p
f- (and d-) orbitals are highly localised
Problem: DFT does not accurately describe f- (and d-) states
Ln dopant in a wide band gap host

## Slide 10: DFT suffers from the derivative discontinuity

## Slide 11: DFT suffers from the derivative discontinuity
The exact exchange-correlation functional is not known.
Problems:

## Slide 12: DFT suffers from the derivative discontinuity
The exact exchange-correlation functional is not known.
Approximate functionals display continuous, concave behaviour.
Problems:

## Slide 13: DFT suffers from the derivative discontinuity
The exact exchange-correlation functional is not known.
Approximate functionals display continuous, concave behaviour.
The lack of derivative discontinuity partly leads to the “band gap problem”.
Problems:

## Slide 14: DFT suffers from the self-interaction error
Notes: In the KS formulation, energy is calculated by solving a series of one-electron equations of the form (seen above).
Kohn-Sham equations are single-electron wave functions that depend on only three spatial variables, psi_i(r).

## Slide 15: DFT suffers from the self-interaction error
The Hartree potential introduces the self-interaction error.
Notes: The Hartree potential describes the Coulomb repulsion between the electron and the system’s total electron density.

## Slide 16: DFT suffers from the self-interaction error
The Hartree potential introduces the self-interaction error.
The exact exchange-correlation potential contains the self-interaction correction.
Notes: The Hartree potential describes the Coulomb repulsion between the electron and the system’s total electron density.

## Slide 17: DFT suffers from the self-interaction error
The Hartree potential introduces the self-interaction error.
The exact exchange-correlation potential contains the self-interaction correction.
Problem: the exact exchange-correlation functional is not known  the self-interaction error remains.
DFT over-delocalises electron density.
Notes: The Hartree potential describes the Coulomb repulsion between the electron and the system’s total electron density.

## Slide 18: DFT suffers from the self-interaction error
e-
e-

## Slide 19: DFT+U – a short summary
DFT+U (simplest) formulation
Notes: This expression has been written for the simplest and most common case of a single subshell nl on site I with associated magnetic quantum numbers, ml, upon which a Hubbard term is applied and a double-counting term that depends on total occupation of that subshell, N Iσ.
EHub is the term that contains the Hubbard Hamiltonian to model correlated states.
Because of the additive nature of this correction, it is necessary to eliminate from the (approximate) DFT functional, ELDA, the part of the interaction energy to be modeled by EHub. This task is accomplished through the subtraction of the so-called “double-counting” (dc) term Edc that models the contribution of correlated electrons to the DFT energy as a mean-field approximation of EHub.
In its general form, DFT+U may be thought of as the net contribution from (1) the standard DFT calculation (EDFT), (2) the Hubbard term (EHub) that explicitly models the Coulomb energy associated with the localized atomic orbitals of interest (e.g., 3d electrons), and (3) removal of a double counting term (EDC) that corresponds to a mean field description of these interactions obtained in the homogeneous electron gas limit with a standard DFT functional.

## Slide 20: DFT+U – a short summary
U – Coulomb parameter
J – exchange parameter
DFT+U (simplest) formulation
U acts to increase localization, decrease the energy of filled states and increase the energy of unfilled states. J does the opposite.
Notes: This expression has been written for the simplest and most common case of a single subshell nl on site I with associated magnetic quantum numbers, ml, upon which a Hubbard term is applied and a double-counting term that depends on total occupation of that subshell, N Iσ.
EHub is the term that contains the Hubbard Hamiltonian to model correlated states.
Because of the additive nature of this correction, it is necessary to eliminate from the (approximate) DFT functional, ELDA, the part of the interaction energy to be modeled by EHub. This task is accomplished through the subtraction of the so-called “double-counting” (dc) term Edc that models the contribution of correlated electrons to the DFT energy as a mean-field approximation of EHub.
In its general form, DFT+U may be thought of as the net contribution from (1) the standard DFT calculation (EDFT), (2) the Hubbard term (EHub) that explicitly models the Coulomb energy associated with the localized atomic orbitals of interest (e.g., 3d electrons), and (3) removal of a double counting term (EDC) that corresponds to a mean field description of these interactions obtained in the homogeneous electron gas limit with a standard DFT functional.

## Slide 21: DFT+U – a short summary
U – Coulomb parameter
J – exchange parameter
DFT+U (simplest) formulation
U acts to increase localization, decrease the energy of filled states and increase the energy of unfilled states. J does the opposite.
Popular simplifying assumption (Dudarev): Ueff = U - J
Notes: This expression has been written for the simplest and most common case of a single subshell nl on site I with associated magnetic quantum numbers, ml, upon which a Hubbard term is applied and a double-counting term that depends on total occupation of that subshell, N Iσ.
EHub is the term that contains the Hubbard Hamiltonian to model correlated states.
Because of the additive nature of this correction, it is necessary to eliminate from the (approximate) DFT functional, ELDA, the part of the interaction energy to be modeled by EHub. This task is accomplished through the subtraction of the so-called “double-counting” (dc) term Edc that models the contribution of correlated electrons to the DFT energy as a mean-field approximation of EHub.
In its general form, DFT+U may be thought of as the net contribution from (1) the standard DFT calculation (EDFT), (2) the Hubbard term (EHub) that explicitly models the Coulomb energy associated with the localized atomic orbitals of interest (e.g., 3d electrons), and (3) removal of a double counting term (EDC) that corresponds to a mean field description of these interactions obtained in the homogeneous electron gas limit with a standard DFT functional.

## Slide 22: DFT+U addresses the self-interaction error
CeO2 with an oxygen vacancy
U enforces localisation of the electron density
B. Himmetoglu et al., International Journal of Quantum Chemistry, 2013, 114, 14–49.
DOS
E
DOS
E
DFT+U
Regular DFT

## Slide 23: DFT+U addresses the derivative discontinuity

## Slide 24: DFT+U addresses the derivative discontinuity
DFT+U addresses these problems

## Slide 25: DFT+U is traditionally applied to d-orbitals
dz2
fz3
Not as much work has been done on f-orbitals as has been done on d-orbitals, especially in the context of lanthanide dopants.

## Slide 26: Test system – Cerium-doped yttrium aluminium garnet – YAG primitive cell
Ydodec
Aloct
Altet
Yttrium aluminium garnet/YAG (Y3Al5O12)
Cubic:

## Slide 27: Test system – Cerium-doped yttrium aluminium garnet – creating a cubic supercell
Yttrium aluminium garnet/YAG (Y3Al5O12)
Conditions:
Minimum length: 10 Å
Max # of atoms: 300
Cubic:
# of atoms: 80

## Slide 28: Test system – Cerium-doped yttrium aluminium garnet – creating a cubic supercell
Yttrium aluminium garnet/YAG (Y3Al5O12)
Conditions:
Minimum length: 10 Å
Max # of atoms: 300
Cubic:
# of atoms: 80
Cubic:
# of atoms: 160
Length: 12.13 Å

## Slide 29: Test system – Cerium-doped yttrium aluminium garnet – doping the cubic supercell
Yttrium aluminium garnet/YAG (Y3Al5O12)
Cubic:
# of atoms: 160
Length: 12.13 Å

## Slide 30: Test system – Cerium-doped yttrium aluminium garnet – doping the cubic supercell
Yttrium aluminium garnet/YAG (Y3Al5O12)
Cubic:
# of atoms: 160
Length: 12.13 Å
Doping here

## Slide 31: Test system – Cerium-doped yttrium aluminium garnet – doping the cubic supercell
Yttrium aluminium garnet/YAG (Y3Al5O12)
Cubic:
# of atoms: 160
Length: 12.13 Å
Triclinic:
# of atoms: 160
Length: 12.13 Å
YAG:Ce
Doping here

## Slide 32: Effect of doping on YAG band structure
Spin up
Spin down
YAG
YAG:Ce (U=5)

## Slide 33: Effect of doping on YAG band structure
Spin up
Spin down
YAG:Ce (U=5)
Valence band
Conduction band
E
Ln 5d (empty)
Ln 4f (filled)

## Slide 34: Density functional theory calculations
General calculation information:
PBEsol
Projector augmented wave (PAW) pseudopotentials
Structure relaxation
  Electronic convergence criterion: 10-7 eV
  Ionic convergence criterion: norm of forces < 1 meV Å-1
DFT+U
  Dudarev (Ueff=U-J)
Material | # of atoms | Plane-wave energy cut-off (eV) | k-point mesh
YAG | 80 | 700 | 2 × 2 × 2
YAG supercell | 160 | 700 | 1 × 1 × 1
YAG:Ce | 160 | 700 | 1 × 1 × 1

## Slide 35: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
YAG valence band
YAG conduction band
E
Ce 5d (empty)
Ce 4f (filled)
One way to get a value of U is to tune it to an experimental parameter.
We chose the valence band maximum to the Ce 4f gap.
 | Approx. energy gaps (eV)
YAG band gap (Slack et al.) | 6.5
YAG band gap (Bok et al.) | 7.8
Ce 4fCBM gap | 3.7
VBMCe 4f gap (Slack et al.) | 2.7
VBMCe 4f gap (Bok et al.) | 3.9

## Slide 36: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
YAG valence band
YAG conduction band
E
Ce 5d (empty)
Ce 4f (filled)
One way to get a value of U is to tune it to an experimental parameter.
We chose the valence band maximum to the Ce 4f gap.
 | Approx. energy gaps (eV)
YAG band gap (Slack et al.) | 6.5
YAG band gap (Bok et al.) | 7.8
Ce 4fCBM gap | 3.7
VBMCe 4f gap (Slack et al.) | 2.7
VBMCe 4f gap (Bok et al.) | 3.9

## Slide 37: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
YAG valence band
YAG conduction band
E
Ce 5d (empty)
Ce 4f (filled)
One way to get a value of U is to tune it to an experimental parameter.
We chose the valence band maximum to the Ce 4f gap.
 | Approx. energy gaps (eV)
YAG band gap (Slack et al.) | 6.5
YAG band gap (Bok et al.) | 7.8
Ce 4fCBM gap | 3.7
VBMCe 4f gap (Slack et al.) | 2.7
VBMCe 4f gap (Bok et al.) | 3.9

## Slide 38: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
YAG valence band
YAG conduction band
E
Ce 5d (empty)
Ce 4f (filled)
One way to get a value of U is to tune it to an experimental parameter.
We chose the valence band maximum to the Ce 4f gap.
 | Approx. energy gaps (eV)
YAG band gap (Slack et al.) | 6.5
YAG band gap (Bok et al.) | 7.8
Ce 4fCBM gap | 3.7
VBMCe 4f gap (Slack et al.) | 2.7
VBMCe 4f gap (Bok et al.) | 3.9

## Slide 39: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
YAG valence band
YAG conduction band
E
Ce 5d (empty)
Ce 4f (filled)
One way to get a value of U is to tune it to an experimental parameter.
We chose the valence band maximum to the Ce 4f gap.
 | Approx. energy gaps (eV)
YAG band gap (Slack et al.) | 6.5
YAG band gap (Bok et al.) | 7.8
Ce 4fCBM gap | 3.7
VBMCe 4f gap (Slack et al.) | 2.7
VBMCe 4f gap (Bok et al.) | 3.9

## Slide 40: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=0
4.3 eV
Filled
Unfilled
Even U=0 shows localization of the Ce 4f state

## Slide 41: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=1
3.9 eV
~3.9 eV is the Bok et al. value

## Slide 42: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=2
3.5 eV

## Slide 43: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=3
2.9 eV

## Slide 44: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=4
2.8 eV
~2.7 eV is the Slack et al. value

## Slide 45: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=5
2.1 eV

## Slide 46: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=6
1.6 eV

## Slide 47: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=7
1.0 eV

## Slide 48: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=8
0.5 eV

## Slide 49: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=9 (not converged)
0.1 eV
U=9 Ce 4f band shows delocalisation

## Slide 50: Tuning U in cerium-doped yttrium aluminium garnet (YAG)
U=1 gives a VBMCe 4f gap of 3.9 eV – this is the Bok et al. value.
U=4 gives a VBMCe 4f gap of 2.8 eV – close to the Slack et al. value of ~2.7 eV.
Since the Slack et al. value is more commonly used, future DFT+U calculations primarily use U=4.
Summary:

## Slide 51: Obtaining U ab initio – the linear response method – Cococcioni et al.
Obtain single point energy and store the charge density.
Bare response : Apply various spherical potential shifts, α, to the subshell of the atom you want to eventually apply the U parameter to (e.g. -0.08-0.08 eV in steps of 0.02 eV) using the charge density from step 1 and keeping it fixed. Collect the occupations of your chosen subshell.
Self-consistent response : repeat step 2 without keeping the charge density fixed.
Plot subshell occupations vs. potential shift and calculate the bare and self-consistent response gradients and respectively.
Calculate U:
General method:

## Slide 52: Obtaining U ab initio – the linear response method – Cococcioni et al.
O (2p)
Y (4d)
Ce (4f)

## Slide 53: Obtaining U ab initio – the linear response method – Cococcioni et al.
1.3 eV
5.0 eV
2.8 eV
Applying U=4 to Ce 4f only
4.4 eV
Applying U values from linear response to O 2p, Y 4d and Ce 4f

## Slide 54: Liechtenstein and Dudarev implementations
Liechtenstein (rotationally invariant) formulation:
Introduced in 1995 as an improvement to the original (rotationally variant/Anisimov) formulation.
Explicitly models the U and J parameters.
Seldon sees use.
Dudarev (simplified) formulation:
‘Simplified’ relative to the Liechtenstein formulation.
Introduced in 1998.
Models the U and J parameters as Ueff.
Preferred DFT+U formulation.

## Slide 55: Dudarev vs. Liechtenstein formulations and metastability issues
YAG:Ce (Ce 4f-subshell)
NiO (Ni 3d-subshell)

## Slide 56: Dudarev vs. Liechtenstein formulations and metastability issues
YAG:Ce (Ce 4f-subshell)
NiO (Ni 3d-subshell)
The differences for YAG:Ce are due to convergence to different states for a given U value.

## Slide 57: U-ramping – Meredig et al.
U-ramping method: Increase U from 0 to a target value in small steps (e.g. 0.1).
U-ramping helps address DFT’s derivative discontinuity problem

## Slide 58: Applying U-ramping to Ce 4f in YAG:Ce
Getting closer to integral occupation.
U-ramping method: Increase U from 0 to a target value in small steps (e.g. 0.1).

## Slide 59: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f-3
Integral occupation of a lead diagonal element corresponds to localisation on a given orbital.
Perform a structure relaxation with occupation matrix control.

## Slide 60: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f-3
Integral occupation of a lead diagonal element corresponds to localisation on a given orbital.
Perform a structure relaxation with occupation matrix control.
Continue from the resultant wavefunction of the previous step and perform another structure relaxation without imposing occupation matrix control.

## Slide 61: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f-3
Resultant occupation nos.

## Slide 62: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f-2
Resultant occupation nos.

## Slide 63: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f-1
Resultant occupation nos.

## Slide 64: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f0
Resultant occupation nos.

## Slide 65: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f1
Resultant occupation nos.

## Slide 66: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f2
Resultant occupation nos.

## Slide 67: Occupation matrix control – Jomard/Amadon/Dorado et al.
Initial occupation matrix
Localisation on f3
Resultant occupation nos.

## Slide 68: U-ramping vs. occupation matrix control
Occupation matrix control does not always find the ground state

## Slide 69: Quasi-annealing – Geng et al.
Simulated annealing is used in molecular dynamics to attempt to find the ground state configuration.
Quasi-annealing applies the principles of simulated annealing to an electronic system.
Notes: In a classical system, the metastable states difficulty can be tackled satisfactorily with annealing procedure. Namely, to remove the thermal kinetic energy of a system gradually and slowly so that all low-lying states have been visited before picking out the ground solution. Similar concept can be applied to electronic system. The basic idea is to shake or heat the electronic system with a spurious energy noise to help it overcome the energy barriers. We call this method the quasiannealing QA procedure.

## Slide 70: Quasi-annealing – Geng et al.
Perform structure relaxations with increasingly stricter electronic convergence criteria and ionic step lengths.
After each structure relaxation, ‘restore’ the structure to the one used prior to performing a structure relaxation.
Once all structure relaxations with the stricter parameters is completed, get the energy per atom of the final structure, then perturb the final structure and use it as the ‘basis of restoration’ for the next set of structure relaxations.
Repeat steps 1-3 until the difference in final structure energies is less than a given tolerance value, e.g. 0.1 meV/atom.
Very vague overview:

## Slide 71: Workflow diagram of my implementation of QA

## Slide 72: Quasi-annealing – Geng et al.
Ideally used after another metastability fixer, such as U-ramping.
Problem: an ionic convergence criterion of 0.01/0.02 eV/Å were used in the quasi-annealing papers. Our calculations stalled when we tried to use such a criterion. We then swapped to an energy-based criterion and had to tweak the amount of distortion for perturbation.
Attempt no. | QA convergence criterion (meV/atom) | Distortion range (Å) | ΔE between UR & QA (eV)
1 | 0.1 | 10-5-10-3 | -0.0001
2 | 0.01 | 10-5-10-2 | +0.152
3 | 0.01 | 10-5-10-2 | +0.153
a.k.a. U-ramping
This method is not reliable
Notes: In a classical system, the metastable states difficulty can be tackled satisfactorily with annealing procedure. Namely, to remove the thermal kinetic energy of a system gradually and slowly so that all low-lying states have been visited before picking out the ground solution. Similar concept can be applied to electronic system. The basic idea is to shake or heat the electronic system with a spurious energy noise to help it overcome the energy barriers. We call this method the quasiannealing QA procedure.

## Slide 73: F-occupation smearing and U-ramping (FOUR) – Rabone and Krack
Set equal occupation nos. for all orbitals throughout a U-ramping run with a step of 0.1.
Continue from the resultant wavefunctions from step 1 and perform a U-ramping run with a step of 0.05 without using occupation matrix control.
Step 1
Step 2

## Slide 74: Summary
Dudarev and Liechtenstein (DFT+U methods)
Linear response method (determining U)
Occupation matrix control (metastability)
U-ramping (metastability)
Quasi-annealing (metastability)
F-occupation and U-ramping (metastability)
Methods and techniques covered so far

## Slide 75: Future work
Use Ilya’s quantum embedding program (if it is ready) to get a more accurate band structure for YAG:Ce.
DFT+U+V
DFT+U+J
SCF linear response method
Applying U to multiple subshells on a given atom
Explore ways to bring down unfilled 5d-orbitals

## Slide 76: Thank you for your attention. Any questions?